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	Product Description
	This Traditional Bonding Liquid is a penetrating, bonding and stabilizing Primer for interior and exterior use on powdery, friable and very porous new and weathered substrates such as lime wash, old paint, new friable or porous plaster and fillers. Once the Bonding Liquid has done its job these areas can be over coated with a range of water and Alkyd based decorative products.



	Application Areas
	· Interior and exterior use.
· New or weathered plaster, hardboard and fibre cement walls.

· Powdery, friable, weathered, previously painted areas.

· Lime wash. 

	Product Features
	· The Bonding Liquid penetrates deep into the substrate and stabilizes it.

· The Bonding Liquid has a good alkaline resistance and can be used on objects where aggressive minerals are present.

· Once sealed can be top coated with a wide range of  Water and Alkyd based products.

· Excellent penetrating and binding properties.

· Excellent adhesion. 

	Product Data
	Resin Base
	Solution Acrylic

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 3-4 hours

	
	Film Thickness
	5-10  microns per coat

	
	Spreading Rate
	10-12 SQM per 1 litre
Although the spreading rate will vary with porosity and type of substrate,

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	· Brush, Roller

	· Thinning
	This Product is ready for use un-thinned; only thin with White Spirits if the substrate is extremely porous.

	· Cleaning
	Application equipment clean up is with White Spirits

	· Application
	· Stir well before use.
· With brush or roller apply a generous coat of Plaster Primer to the area that needs protecting.
· Allow to dry 4-6 hours before recoating.
· Clean tools immediately after use with White Spirits.

· Do not apply before 09:00 and after 16:00 in the winter.
· Do not apply exterior if it looks like rain will occur with in 4-6 hours of application.

	Surface Preparation
	

	· Uncoated dry porous concrete surfaces
	· Remove dust, foreign material, fungal and algae growth.

· Seal with Bonding Liquid.


	· Raw Plaster
	· Remove dust, foreign material, fungal and algae growth.

· Seal with Bonding Liquid.

	· Uncoated, Weathered or New Fibre Cement Surfaces
	· Remove dust, foreign material, fungal and algae growth.

· Seal with Bonding Liquid.

	· Previously Painted Surfaces
	· Remove all loose, flaking and bubbling paint.

· Remove all dust, foreign material, fungal and algae growth.

· Lime wash coated walls: remove lime wash as far as possible with scraper blades and / or soft wire or hard fibre brushes but be careful not to damage the plaster.

· Allow to dry.

· Fill and seal all visible cracks.
· Sand well and remove dust.

· Seal with Bonding Liquid.

	Colour Range and Quantities
	· Clear 
· Available in 1,5 and 20 litres.

	Precautions
	· This Product is  flammable, Flash Point 37 Deg C 

	Disclaimer
	Dynamiq Intelligent Coatings cannot be held liable if the product fails due to improper surface preparation or application.
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