| Product Description | Heat Reflective (Infra-Red) Chicken House Paint |  |
| --- | --- | --- |
| Application Areas | - Primed Wood/Metal. - Primed Cement Plaster or Fibre Cement. - Previously Painted Substrates. - Roofs. |  |
| Product Features | - A new generation pure acrylic long life heat reflecting (Infra-Red) roof paint. - High durability and UV resistance against the harsh Gauteng climate. - Water resistant. - Infra-Red heat reflection. - Excellent adhesion and flexibility. - Easy no-mess application properties. - Quick drying - 2 coats can be applied in one day. - When correctly applied to a properly prepared substrate, the product has a life expectancy of 10 years - possibly longer. The use of Specialized Polymers improves durability, water-resistance, dirt-shedding as well as reflecting heat and reducing under-roof temperature. |  |
| Product Data | Resin Base | Acrylic resin emulsion |
|  | Drying Time | Touch dry: ± 1 hour Hard dry: ± 4 - 6 hours |
|  | Film Thickness | 70-90 microns per coat |
|  | Spreading Rate | 6 - 8 sqm per litre per coat. NOTE: Spreading rate can vary due to substrate porosity and substrate type. For uncoated new surfaces work on 3-4 sqm/1L for the first coat and 4-5 sqm/1L for subsequent coats and when applied to sealed or previously painted substrates. |
| Application Details |  |  |
| - Mixing | Always stir well to a smooth consistency before use with a flat paddle. |  |
| - Application Method | Brush, Roller and Airless Spray |  |
| - Thinning | This Product is ready for use un-thinned; thinning with water will reduce its hiding ability and efficacy (life-span). |  |
| - Cleaning | Clean application equipment thoroughly with clean tap water. |  |
| - Application | - Stir well before use. - With a brush or roller apply a generous coat of CHIRP to the area that needs protecting. - Allow to dry 3-4 hours before recoating. - With a brush or roller apply a second generous coat. - A minimum of 2 coats of CHIRP are required for best results. - Do not thin the product – use as applied. Do not exceed recommended spreading rate - Do not apply before 09:00 and after 16:00 in the winter. - Do not apply on exposed exterior surfaces if rain is imminent within 4-6 hours of application. |  |
| Surface Preparation |  |  |
| - Rusted Metal | - Remove loose dirt, sand and dust from the area. - Affected areas need to be cleaned back to bright metal and spot primed with a lightly coloured water-based rust-retarding primer. - If required wash, rinse and dry the surface before application. - Apply at least 2 coats of CHIRP. |  |

| - New Metal | - Surfaces MUST be degreased with a Galvanized Iron Cleaner to remove the manufacturer’s grease protective layer. Repeat the process until the surface is water-break free. - Rinse well with potable water. - Prime the clean degreased metal with a lightly coloured water-based rust-retarding primer. - Apply at least 2 coats of CHIRP. |
| --- | --- |
| - Wood | - Sand smooth and wipe off all dust. - Prime with Synthetic Universal Undercoat. - Apply at least 2 coats of CHIRP. |
| - Uncoated cement plaster surfaces | - Remove dust and foreign material. - Remove all fungal and algae growth with bleach until clean. - Fill all visible cracks with an appropriate Crack Filler, allow to dry then seal with an alkali-resistant primer. - Apply at least 2 coats of CHIRP. |
| - Fibre Cement Surfaces (Uncoated, Weathered or New) | - Remove dust, foreign material. - Remove all fungal and algae growth with bleach until clean. - If friable or powdery, seal with a bonding liquid or alkali-resistant primer. - Apply at least 2 coats of CHIRP. |
| - Previously painted surfaces | - Make sure old paint coatings are firm and solid. - Remove all loose, flaking and bubbling paint. - Remove all dust, grease and foreign material. - Remove all fungal and algae growth with bleach until clean. - If friable or powdery, seal with a bonding liquid or alkali-resistant primer. - Dark coloured paint might require a suitable white undercoat before applying CHIRP. - Apply at least 2 coats of CHIRP. |
| Colour range and quantities | - Due to its reflective properties this product is only available in white. - Available in 5 and 20 litres. |
| Precautions | - CHIRP is not flammable, contains no toxic substances and very low levels of VOC meeting EU regulations. |