TECHNICAL DATA SHEET



	Product Description
	Heat Reflective (Infra-Red) Chicken House Paint

	Application Areas
	· Primed Wood/Metal.
· Primed Cement Plaster or Fibre Cement.
· Previously Painted Substrates.
· Roofs.

	Product Features
	· A new generation pure acrylic long life heat reflecting (Infra-Red)  roof paint.
· High durability and UV resistance against the harsh Gauteng climate.
· Water resistant.
· Infra-Red heat reflection.
· Excellent adhesion and flexibility.
· Easy no-mess application properties.
· Quick drying - 2 coats can be applied in one day.
· When correctly applied to a properly prepared substrate, the product has a life expectancy of 10 years - possibly longer. The use of Specialized Polymers improves durability, water-resistance, dirt-shedding as well as reflecting heat and reducing under-roof temperature.

	Product Data
	Resin Base
	Acrylic resin emulsion

	
	Drying Time
	Touch dry: ± 1 hour Hard dry: ± 4   - 6 hours

	
	Film Thickness
	70-90 microns per coat

	
	Spreading Rate
	[bookmark: _GoBack]6 - 8 sqm per litre per coat.
NOTE: Spreading rate can vary due to substrate porosity and substrate type. For uncoated new   surfaces work on 3-4 sqm/1L for   the first coat and 4-5 sqm/1L for
subsequent coats and when applied to   sealed or previously painted substrates.

	Application Details
	

	· Mixing
	Always stir well to a smooth consistency before use with a flat paddle.

	· Application Method
	Brush, Roller and Airless Spray

	· Thinning
	This Product is ready for use un-thinned; thinning with water will reduce its hiding ability and efficacy (life-span).

	· Cleaning
	Clean application equipment thoroughly with clean tap water.

	· Application
	· Stir well before use.
· With a brush or roller apply a generous coat of CHIRP to the area that needs protecting.
· Allow to dry 3-4 hours before recoating.
· With a brush or roller apply a second generous coat.
· A minimum of 2 coats of CHIRP are required for best results.
· Do not thin the product – use as applied. Do not exceed recommended spreading rate
· Do not apply before 09:00 and after 16:00 in the winter.
· Do not apply on exposed exterior surfaces if rain is imminent within 4-6 hours of   application.

	Surface Preparation
	

	· Rusted Metal
	· Remove loose dirt, sand and dust from the area. 
· Affected areas need to be cleaned back to bright metal and spot primed with a lightly coloured water-based rust-retarding primer.
· If required wash, rinse and dry the surface before application.
· Apply at least 2 coats of CHIRP.


	· New Metal
	· Surfaces MUST be degreased with a Galvanized Iron Cleaner to remove the manufacturer’s grease protective layer. Repeat the process until the surface is water-break free.
· Rinse well with potable water.
· Prime the clean degreased metal with a lightly coloured water-based rust-retarding primer.
· Apply at least 2 coats of CHIRP.

	· Wood
	· Sand smooth and wipe off all dust.
· Prime with Synthetic Universal Undercoat.
· Apply at least 2 coats of CHIRP.

	· Uncoated cement plaster surfaces
	· Remove dust and foreign material. 
· Remove all fungal and algae growth with bleach until clean.
· Fill all visible cracks with an appropriate Crack Filler, allow to dry then seal with an alkali-resistant primer.
· Apply at least 2 coats of CHIRP.

	· Fibre Cement Surfaces (Uncoated,
       Weathered or    
       New)
	· Remove dust, foreign material.
· Remove all fungal and algae growth with bleach until clean.
· If friable or powdery, seal with a bonding liquid or alkali-resistant primer.
· Apply at least 2 coats of CHIRP.

	· Previously painted   surfaces
	· Make sure old paint coatings are firm and solid.
· Remove all loose, flaking and bubbling paint.
· Remove all dust, grease and foreign material.
· Remove all fungal and algae growth with bleach until clean.
· If friable or powdery, seal with a bonding liquid or alkali-resistant primer.
· Dark coloured paint might require a suitable white undercoat before applying CHIRP.
· Apply at least 2 coats of CHIRP.

	Colour range and quantities
	· Due to its reflective properties this product is only available in white.
· Available in 5 and 20 litres.

	Precautions
	· CHIRP is not flammable, contains no toxic substances and very low levels of VOC meeting EU regulations.
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