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	Product Description
	A new generation Alkyd Resin interior semi-gloss floor coating for those high traffic areas that need a highly washable, alkali and abrasion resistant coating in a range of colours. 

	Application Areas
	· Dry (moisture level 6% Max) cement/Concrete floors. 

· Primed metal and wooden substrates.

	Product Features
	· Highly washable, cleanable, humidity and abrasion resistant.
· Excellent adhesion to range of properly prepared, dry flooring substrates.
· Excellent, no mess application properties, with excellent, flow and leveling.
· High hiding power and film build .
· Alkali resistant when applied to dry cement floors (moisture level 6% max).

	Product Data
	Resin Base
	Synthetic Alkyd resin

	
	Drying Time
	Touch dry: 3-4 hours
Hard dry: 10-12hours

	
	Film Thickness
	± 30 microns

	
	Spreading Rate
	 7-9 SQM per 1 litre
Although the spreading rate will vary with porosity and type of substrate, for uncoated new surfaces work on 6-8 square metres per litre for the first coat and  9-11square metres per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	
	Surface Appearance
	Semi Gloss

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	Brush, roller or spray application.

	· Thinning
	This is ready for use un-thinned; thinning with Turpentine will reduce its hiding power.

	· Cleaning
	Application equipment cleanup is with Turpentine/White Spirits

	· Application
	· With brush, roller or spray  apply a generous coat of Dynamiq Enamel Concrete Paint to the area that needs protecting.
· Allow to dry overnight before recoating.
· Do not apply before 09:00 and after 16:00 in the winter.

	Surface Preparation
	

	· Rusted Metal
	· Remove any rust and mill scale from steel surface.

· Affected areas need to be cleaned back to bright metal 

· Apply one coat of Dynamiq Zinc Phosphate Primer leave to dry over night

· Apply a coat of Dynamiq Concrete Enamel Paint and allow to dry over-night.
· Apply a second coat. Subsequent coats can be applied if required.

	· New Metal (Galvanized Steel)
	· Degrease surfaces with an abrasive/industrial degreaser to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water-break free.

· After drying apply one coat of water based metal primer, leave to dry overnight

· Apply a coat of Dynamiq Enamel Concrete Paint, allow to dry overnight.
· Apply a second coat. Subsequent coats can be applied if required.


	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid.

· Remove all loose, flaking and bubbling paint.

· Remove all dust, grease, foreign material, fungal and algae growth.

· Spot Prime with Dynamiq Enamel Concrete Paint thinned 5% with Turpentine/White Spirits
· Apply one coat of Dynamiq Enamel Concrete Paint and allow to dry overnight.
· Apply a second coat.

	· Wood and Wood Fibre Boards
	· Sand surface until smooth.

· Apply one coat of Dynamiq Concrete Enamel Paint allow to dry overnight.
· Apply a second coat.

	· Concrete/Cement 

          Floors
	· Dry (6% moisture Max) uncoated concrete surfaces: Remove all dust, foreign material, Fungal, algae growth- fill and seal all visible cracks with a suitable flexible sealant.
· Apply the first coat Thinned 10% with White spirits Allow to dry overnight.
· Apply a second coat.

	Colour Range and Quantities
	· A limited range of ready mixed colours (Grey, Black, Red Oxide; Green)
· Available in 1, 5 and 20 litres. 

	Precautions
	· This product is flammable.

· Use only in well ventilated areas.

· Do not eat, drink or smoke while applying.
· This product continues no toxic substances.

	Disclaimer
	Dynamiq Intelligent Coatings cannot be held liable if the product fails due to improper surface preparation or application.
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