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	Product Description
	Dynamic Exterior Acrylic Sheen. 

	Application Areas
	· Primed Wood/Metal.
· Primed Cement Plaster or Fibre-Cement. 
· Previously painted substrates.
· Mostly exterior but works well for interior walls. 

	Product Features
	· This product is a new generation all acrylic long life highly washable sheen paint.
· Highly water and stain resistant, excellent polish resistance. 
· Excellent adhesion/flexibility.
· Excellent, no mess application properties.
· Low odour.
· Quick drying 2 coats can be applied in one day.
· Meets most of the Performance Criteria of SABS 1586 Grade 1. 

· If correctly applied to a properly prepared substrate, the product has a life expectancy of 7-10 years, possibly longer. The use of a special polymer not only improves washability but  also properties like water/polish resistance and dirt shedding. 

	Product Data
	Resin Base
	Acrylic resin emulsion

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 4-6 hours

	
	Film Thickness
	30-40  microns per coat

	
	Spreading Rate
	9-11 SQM per 1 litre per coat.
NOTE: Spreading rates will vary with porosity and type of substrate. For uncoated new surfaces work on 8-10 square meters per litre for the first coat and 10-12 square meters per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle to a smooth consistency.

	· Application Method
	· Brush, Roller and Airless Spray.

	· Thinning
	This product is ready for use un-thinned; thinning with water will reduce its hiding power and longevity.

	· Cleaning
	Application equipment clean up is with clean tap water.

	· Application
	· Stir well before use.
· With brush or roller apply a generous coat of Dynamiq Exterior to the area that needs protecting.
· Allow to dry 3-4 hours before recoating.
· With a brush or roller apply a second generous coat.
· 2 Coats of Dynamiq Exterior are used for best results.
· Ready-for-use. DO NOT THIN.
· Clean tools immediately after use with clean tap water.
· Do not apply before 09:00 and after 16:00 in the winter.
· Mostly exterior.

	Surface Preparation
	

	· Rusted Metal
	· Affected areas need to be cleaned back to bright metal and spot primed with water-based metal primer.
· Remove collected sand and dust from the area.
· Apply two coats of Dynamiq Exterior.


	· New Metal
	· Degrease surfaces with a Galvanized Iron Cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free.
· Rinse well with potable water.
· Prime  the clean degreased metal with a water based metal primer.
· Apply two coats of Dynamiq Exterior. 

	· Wood 
	· Prime with  synthetic universal under coat.
· Lightly sand, wipe off dust.
· Apply two coats of Dynamiq Exterior.

	· Uncoated cement Plaster surfaces
	· Remove dust, foreign material, fungal and algae growth.
· Fill all visible cracks and seal with  Alkali Resistant Primer.
· Apply two coats of Dynamiq Exterior.

	· Fibre Cement Surfaces (Uncoated, Weathered or New)
	· Remove dust, foreign material, fungal and algae growth.
· If friable or powdery, seal with bonding liquid or  alkali resistant primer.
· Apply two coats of Dynamiq Exterior.

	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid.
· Remove all loose, flaking and bubbling paint.
· Remove all dust, grease, foreign material, fungal and algae growth.
· Allow to dry.
· If then powdery or friable, seal with bonding liquid or alkali resistant primer. 
· Apply two coats of Dynamiq Exterior.

	Colour Range and Quantities
	· This product is available in white and a large range of  colours .
· Available in 1, 5 and 20litres.

	Precautions
	· This product is not flammable, contains no toxic substances and only low levels of VOC (EU regulations).

	Disclaimer
	Dynamiq intelligent coatings cannot be held liable if the product fails due to improper surface preparation or application.
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