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	Product Description
	Dynamiq FibreSkin is a new generation water-based acrylic elastic long-life water-proof sealer for roofs, window ledges and parapet walls.

	Application Areas
	· Exterior and interior surfaces.

· Cement Tiles (new or weathered), Fibre Cement sheeting (new or weathered). 
· Primed plaster. 
· Previously painted substrates.

· Primed metal and wooden substrates.

· Flat cement/concrete roofs and walls. 

· Nail heads and roofing bolts and roof tile ridges.  

	Product Features
	· FibreSkin is a fibre-filled coatings material designed to prevent water penetration into the substrate. Applied in several layers it forms a thick protective water-proof skin.

· Available in several popular roof shades as well as white.

· This product contains Fibrous particles combined with a flexible  water-resistant acrylic polymer emulsion.

· Applied to specification it seals Masonry Substrates and prevents water penetration.

· FibreSkin remains highly flexible for years even after extended exposure to the environment.

· Suitable for concrete and tiled roofs, galvanised sheeting, roofing felt and fibre cement, exposed bricks and cement building blocks.
· Ideal for repair work on roofs: sealing nail heads, leaking flashings, cracked roof tiles and roof ridging, repairing damaged or cracked roofing felt.

· Seals window ledges and parapet wall tops.
· Highly durable and UV resistant.

· Waterproof.

· Excellent long-term flexibility.

· Excellent adhesion.

· Easy no-mess application properties.

· Quick drying - 2 coats can be applied in one day.

· Low Odour.

· 2 coats of FibreSkin are used for best results.

· In white and pastel colours it also has the added benefit of reflecting heat and therefore contributes to heat reduction (especially for metal roofs). 

	Product Data
	Resin Base
	Acrylic resin emulsion

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 4-6 hours

	
	Film Thickness
	80-100  microns per coat

	
	Spreading Rate
	2  SQM per 1 litre

Although the spreading rate will vary with porosity and type of substrate, for uncoated new surfaces work on 0.5-1 square meters per litre for the first coat and 1.5 -2 square meters per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	· Brush, roller or trowel

	· Thinning
	This Product is ready for use un-thinned; thinning with water will reduce its hiding power.

	· Cleaning
	Application equipment clean up is with clean tap water.

	· Application
	· Stir well before use.

· With brush or roller, apply a generous/thick coat of FibreSkin to the area that needs protecting in small manageable sections.

· Allow to dry 4-6 hours before recoating.

· Apply a second, third and possibly a fourth generous coat, waiting 4-6 hours between coats, until the membrane is totally saturated and the surface has an even and very noticeable high sheen.

· This product is ready for use un-thinned; thinning with water will reduce its hiding power and effectiveness.

· Three to four coats of this product are used for best results.

· Application equipment clean up is with clean tap water.

· Do not apply before 09:00 and after 16:00 in the winter.

· Do not apply exterior if it looks like rain will occur within 4-6 hours of application.

	Surface Preparation
	

	· Rusted Metal
	· Affected areas need to be cleaned back to bright metal and spot primed with water based metal primer. 
· Remove collected sand and dust from the area.

· Apply 2-4 coats of FibreSkin.

	· New Metal
	· Degrease surfaces with a galvanized iron cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free.

· Rinse well with potable water.

· Prime the clean degreased metal with a water based metal primer.
· Apply 2-4 coats of FibreSkin. 

	· Uncoated Cement Plaster Surfaces
	· Remove dust, foreign material, fungal and algae growth.

· Fill all visible cracks and seal with plaster primer.

· Apply 2-4 coats of FibreSkin. 

	· Fibre Cement Surfaces (Uncoated, Weathered or New)
	· Remove dust, foreign material, fungal and algae growth.

· If friable or powdery, seal with bonding liquid or plaster primer.
· Apply 2-4 coats of FibreSkin.

	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid.

· Remove all loose, flaking and bubbling paint.

· Remove all dust, grease, foreign material, fungal and algae growth.

· Allow to dry.

· If then powdery or friable, seal with bonding liquid or plaster primer. 
· Apply 2-4 coats of FibreSkin.

	Colour Range and Quantities
	· This product is available in white and a  range of  colours.   
· Available in 1.5 and 20 litres.

	Precautions
	· This Product is not flammable, contains no toxic substances and only low levels of VOC (EU regulations).

	Disclaimer
	Dynamic Intelligent Coatings cannot be held liable if the product fails due to improper surface preparation or application.


	DYNAMIQ
	FIBRESKIN  TDS ISSUE                            May 2021

                                                           Page 1 of 2



[image: image2.png]DYNAM

INTELLIGENT COATINGS



