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	Product Description
	Dynamic GP Acrylic  is cost-effective water based, 10 000 scrub, high opacity matt paint for those areas where you want a matt finish to cover marks and imperfections.

	Application Areas
	· Primed wood/metal.
· Primed cement plaster or fibre-cement.
· Previously painted substrates.

	Product Features
	When applied correctly this product has up to 5 years of life expectancy (normal environmental conditions).
· High opacity.
· Good scrub resistance.
· Excellent, no mess application properties.
· Low odour.
· Quick drying - 2 coats can be applied in one day.

	Product Data
	Resin Base
	Acrylic resin emulsion

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 4-6 hours

	
	Film Thickness
	25-35  microns per coat

	
	Spreading Rate
	6-8SQM per 1 litre per coat.
NOTE: The spreading rate will vary with porosity and type of substrate. For uncoated new surfaces work on 5-7 square meters per litre for the first coat and 7-9 square meters per litre for subsequent coats and for when applied to sealed and previously painted substrates.

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle to a smooth consistency.

	· Application Method
	· Brush, roller and airless spray.

	· Thinning
	This product is ready for use un-thinned; thinning with water will reduce its hiding power and longevity.

	· Cleaning
	Application equipment clean up is with clean tap water.

	· Application
	· Stir well before use.
· With brush or roller apply a generous coat of Dynamiq GP Acrylic to the area that needs protecting.
· Allow to dry 2-3 hours before recoating.
· With a brush or roller apply a second generous coat.
· 2 Coats of this product are used for best results.
· Ready-for-use as supplied. DO NOT THIN.
· Clean tools immediately after use with clean tap water.
· Do not apply before 09:00 and after 16:00 in the winter.


	Surface Preparation
	

	· Rusted Metal
	· Affected areas need to be cleaned back to bright metal and spot primed with a water-based metal primer.
· Remove collected sand and dust from the area.
· Apply two coats of Dynamiq GP Acrylic.


	· New Metal
	· Degrease surfaces with a galvanized iron cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water-break free.
· Rinse well with potable water.
· Prime the clean degreased metal with a water-based metal primer.
· Apply two coats of Dynamiq GP Acrylic.

	· Wood 
	· Prime with a solvent-based universal under coat.
· Lightly sand and wipe off dust.
· Apply two coats of Dynamiq GP Acrylic.

	· Uncoated Cement Plaster Surfaces
	· Remove dust, foreign material, fungal and algae growth.
· Fill all visible cracks and seal with plaster primer.
· Apply two coats of Dynamiq GP Acrylic.

	· Fibre Cement Surfaces (Uncoated, Weathered or New)
	· Remove dust, foreign material, fungal and algae growth
· If friable or powdery, seal with bonding liquid or alkali resistant primer.
· Apply two coats of Dynamiq GP Acrylic. 

	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid.
· Remove all loose, flaking and bubbling paint.
· Remove all dust, grease, foreign material, fungal and algae growth.
· Allow to dry.
· If surface is powdery or friable, seal with bonding liquid or plaster primer.
· Apply two coats of Dynamiq GP Acrylic.

	Colour Range and Quantities
	· This product is available in white and standard colours. Dynamiq GP Acrylic van be tinted to bespoke colours.
· Available in 5 and 20litres containers.

	Precautions
	· This product is not flammable, contains no toxic substances and only low levels of VOC (EU regulations).
· This product must not be used as a replacement for plaster primer as it will fail in this role.

	Disclaimer
	Dynamiq Intelligent Coatings and its manufacturers cannot be held liable if the product fails due to improper surface preparation or application.
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