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	Product Description
	This traditional pigmented Plaster Primer is a penetrating, bonding and stabilizing primer for interior and exterior use on powdery, friable and very porous new and weathered substrates such as lime wash, old paint, new friable or porous plaster and fillers. Once the Dynamiq Plaster Primer has done its job these areas can be over coated with a range of paints - Water and Alkyd based decorative products.



	Application Areas
	· Interior and exterior use.
· New or weathered plaster, hardboard and fibre-cement walls.
· Powdery, friable, weathered, previously painted areas.
· Lime wash.

	Product Features
	· The Primer penetrates deep into the substrate and stabilizes it.
· Dynamiq Plaster Primer has a good alkaline resistance and can be used on objects where aggressive minerals are present.
· Once sealed, it can be top coated with a wide range of Water and Alkyd based paints.
· Excellent penetrating and binding properties.
· Excellent adhesion.

	Product Data
	Resin Base
	Solution Acrylic

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 3-4 hours

	
	Film Thickness
	30-40  microns per coat

	
	Spreading Rate
	6-8  SQM per 1 litre
Although the spreading rate will vary with porosity and type of substrate.

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle to a smooth consistency.

	· Application Method
	· Brush, Roller

	· Thinning
	This product is ready for use un-thinned; only thin with White Spirits if the substrate is extremely dense. 

	· Cleaning
	Application equipment clean up is with White Spirits/Turpentine.

	· Application
	· Stir well before use.
· With brush, roller apply a generous coat of Dynamiq Plaster Primer to the area that needs protecting.
· Allow to dry 4-6 hours before recoating.
· Clean tools immediately after use with White Spirits.
· Do not apply before 09:00 and after 16:00 in the winter.
· Do not apply exterior if it looks like rain will occur with in 4-6 hours of application.
· Do not apply to damp surfaces.

	Surface Preparation
	

	· Uncoated Dry Porous Concrete Surfaces
	· Remove dust, foreign material, fungal and algae growth.
· Seal with Dynamiq Plaster Primer.


	· Raw Plaster
	· Remove dust, foreign material, fungal and algae growth.
· Seal with Dynamiq Plaster Primer.

	· Uncoated, Weathered or New Fibre Cement Surfaces
	· Remove dust, foreign material, fungal and algae growth.
· Seal with Dynamiq Plaster Primer.

	· Previously Painted Surfaces
	· Remove all loose, flaking and bubbling paint.
· Remove all dust, foreign material, fungal and algae growth.
· On Lime-wash coated walls, remove the lime wash as far as possible with scraper blades and / or soft wire or hard fibre brushes being careful not to damage the plaster.
· Allow to dry.
· Fill and seal all visible cracks. 
· Sand well and remove dust.

· Seal with Dynamiq Plaster Primer. 

	Colour Range and Quantities
	· White 
· Available in 1,5 and 20 litres

	Precautions
	· This Product is flammable, Flash Point 37 Deg C 

	Disclaimer
	Dynamiq Intelligent Coatings and its Manufacturers cannot be held liable if the product fails due to improper surface preparation or application.
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