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	Product Description
	A classic single pack, urethane alkyd based, long-life, interior, abrasion resistant, high gloss coating for those high traffic areas that need a highly abrasion, water and chemical resistant coating in a range of colours.

	Application Areas
	· Dry plaster or concrete substrates.
· Primed metal and wooden substrates.

· It is ideal to protect floors in an aggressive environment for example factories where aggressive chemicals are used and in food processing plants.
· Interior use only.

	Product Features
	· Highly abrasion and chemical resistant.

· Highly washable and cleanable.

· Excellent adhesion to range of properly prepared substrates.

· Excellent, no mess application properties with excellent flow and leveling.

· High hiding power and film build.

· Dynamiq Polyurethane Floor Paint forms a very hard and dense coating. It is resistant against alkalis, mild acids, water and mineral oil substances.
· 1 Coat of Polyurethane Clear Floor Sealer/Primer and 2 coats of Polyurethane Floor Paint are used for best results.

· Urethane alkyd based coatings are not suitable for exterior use since they will deteriorate /Crack in UV light.
· Dynamiq Polyurethane Floor Paint can be applied on existing gloss or semi gloss enamel paints if they are clean/grease free and lightly sanded. 

	Product Data
	Resin Base
	Urethane Modified Alkyd 

	
	Drying Time
	Drying time is temperature related. At room temperature:
Touch dry: 2-3 hours

Hard dry:/recoating Time 16 hours

	
	Film Thickness
	± 35 microns

	
	Spreading Rate
	8 - 10 SQM per litre per coat.
NOTE: Spreading rates will vary with porosity and type of substrate. For uncoated new surfaces work on 6-8 square metres per litre for the first coat and 10-12 square metres per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	
	Surface Appearance
	Gloss finish

	Application Details
	

	· Mixing
	Stir paint well before use with a flat paddle.

	· Application Method
	With brush, mohair paint roller or airless spray.

	· Thinning
	Mineral Turps 

	· Cleaning
	Clean up application equipment with Mineral Turps 

	· Application
	· Stir well before use.
· With brush, mohair roller or airless spray, apply a generous coat of Dynamiq Polyurethane Floor Paint to the area that needs protecting. For spray application, thin to 20-25 seconds. No. 4 Ford cup with Mineral Turps .
· Allow to dry 18-24 hours (24-48 Hours in cold winter weather) but no longer than 48 hours, before recoating.
· With brush, mohair roller or airless spray, apply a second generous coat Dynamiq Polyurethane Floor Paint.
· Clean up application equipment with Mineral Turps. 
· 1 coat of Polyurethane Clear Sealer/ Primer 2 Coats of Dynamiq Polyurethane Floor paint are used for best results.

· Urethane Alkyd Based coatings must be used within a strict time sequence. Each coating must be applied 24 hours after the previous one otherwise there will be no proper bond between the coatings.

· Only apply in well ventilated areas.

· Keep away from all ignition sources, flames and sparks.

· Do not eat drink or smoke while applying.

· Do not apply before 09:00 and after 16:00 in the winter.

	Surface Preparation
	

	· Rusted Metal / Mild Steel
	· Affected areas need to be cleaned back to bright metal and spot primed with Etch Primer.

· Apply two coats of Dynamiq Polyurethane Floor Paint. 

	· New Metal
	· Degrease surfaces with Galvanized Cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free.

· After drying, the whole substrate is coated with Etch Primer.

· Apply two coats of Dynamiq Polyurethane Floor Paint.

	· Dry, Uncoated and New Concrete Surfaces
	· Make sure concrete is firm and completely dry. Plaster or concrete must be completely dry as water vapour cannot permeate through Urethane Alkyd Based coatings.

· Remove all dust, foreign material, fungal, algae growth.

· Fill and seal all visible cracks and coat with Dynamiq Polyurethane Clear Primer/Sealer. 
· Apply two coats of Dynamiq Polyurethane Floor Paint in the required colour 

	· Raw / New Plaster
	· Make sure plaster is firm and completely dry.

· Remove all dust, foreign material, fungal and algae growth.

· Fill all visible cracks with Crack Filler
· Fill and seal all visible cracks and coat with Polyurethane Clear Primer/Sealer. 

· Apply two coats of Dynamiq Polyurethane Floor paint. In the required colour.

	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid.

· Remove all loose, flaking and bubbling paint.

· Remove all dust, grease, foreign material, fungal and algae growth.

· Polyurethane Floor Paint does not adhere well on hard and fully cured Alkyd Based coatings. The old coating must be prepared by sanding the product well to a matt and slightly rough surface.
· After drying over night all primed areas and previously painted areas must then be undercoated with Dynamiq Polyurethane Floor Paint.
· Apply 1-2 further coats of Dynamiq Polyurethane Floor Paint.
· Epoxy Floor paint cannot be applied on existing gloss or semi gloss enamel paints.

	Colour Range and Quantities
	· Dynamiq Polyurethane Floor paint is available in a Clear /Primer Sealer and a limited range of popular ready mixed colours.

· Other shades are available on request in minimum batch quantities.
· Available in 1 litre/5 litres and 20 Litres.

	Precautions
	· This material is highly flammable.
· Use only in well ventilated areas and do not eat, drink or smoke during application.

	Disclaimer
	Dynamiq Intelligent Coatings and its Manufacturers cannot be held liable if the product fails due to improper surface preparation or application.
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