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	Product Description
	A classic modified alkyd-based interior, exterior low sheen road marking finish for unpainted bricks, cement, concrete, stone, bituminous and tarmac road surfaces to protect substrates from abrasion, rain and sun. Meets the rigorous requirements of SABS 731 Type 1

	Application Areas
	· Bricks, cement, concrete, stone, bituminous and tarmac road surfaces on roads, airfields, parking areas and driveways.

	Product Features
	· High abrasion resistance and durability.

· Excellent adhesion to a range of properly prepared road surface types.

· Meets SABS 731 standards.

· Suitable for machine application as well as with a paint roller or brush.

· Serves as a base coating for the application of reflective glass beads.

· Available in the different shades required by municipalities and road authorities.

· 1-2 Coats of Dynamiq Road Marking Paint is used for best results.

	Product Data
	Resin Base
	Synthetic Alkyd resin

	
	Drying Time
	Touch dry: 15-20 Minutes
Hard dry: 1-2 hours

	
	Film Thickness
	± 200 microns

	
	Spreading Rate
	 4-6 SQM per 1 litre
Although the spreading rate will vary with porosity and type of substrate, for uncoated new surfaces work on 2-4 square metres per litre for the first coat and 6-8 square metres per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	
	Surface Appearance
	Low sheen 

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	Brush, roller or spray application.

	· Thinning
	This is ready for use un-thinned; thinning with Solumix will reduce its hiding power.

	· Cleaning
	Application equipment clean-up is with Solumix

	· Application
	· Stir well before use.

· With brush, roller or spray, apply a generous coat of Dynamiq Road Marking Paint to the area that needs protecting.

· Allow to dry 1-2 hours before recoating.

· With brush, roller or spray, apply further generous coats if required.
· Solumix should be added only in case of machine application.

· 1-2 coats of Dynamiq Road Marking Paint are used for best results.
· Clean up application equipment with Solumix.
· Only apply in well ventilated areas.

· This material is highly flammable. Keep away from all ignition sources, flames and sparks.

· Do not eat drink or smoke while applying.

· Do not apply before 09:00 and after 16:00 in the winter.

· Do not apply exterior if it looks like rain will occur within 2-3 hours of application.


	Surface Preparation
	

	· Uncoated Concrete, Cement, Stone and Brick Surfaces
	· Substrate must be completely dry and free of dust.

· Remove all dust, foreign material, fungal or algae growth. Fill and seal all visible cracks.

· Remove any old flaking paint coatings.

· Apply one coat of Dynamiq Road Marking Paint to cover substrate well.

· For use on concrete, two applications are recommended.

	· Tarmac and Bitumen
	· Substrate must be completely dry and free of dust.

· Remove all dust, foreign material, fungal or algae growth. Fill and seal all visible cracks.

· Remove any old flaking paint coatings.

· Apply one coat of Dynamiq Road Marking Paint to cover substrate well.

	· Previous road markings
	· Substrate must be completely dry and free of dust.

· Remove all dust, foreign material, fungal or algae growth. Fill and seal all visible cracks.

· Remove any old flaking paint coatings.

· Apply one coat of Dynamiq Road Marking Paint to cover substrate well.

	Colour Range and Quantities
	· Available in white, yellow, green, red and black.

· Available in 1 litre, 5 litres 20 litres and 200 litres.

	Precautions
	· This product is flammable.

· Use only in well ventilated areas.

· Do not eat, drink or smoke while applying.
· This product continues no toxic substances.

	Disclaimer
	Dynamiq Intelligent Coatings cannot be held liable if the product fails due to improper surface preparation or application.
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