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INTELLIGENT COATINGS





	Product Description
	Dynamiq Rubbertex is a versatile, single pack non-slip textured rubber and resin bakkie liner for the load beds and tail lifts of bakkies, 4x4’s, trucks and trailers. It can also be used to create non-slip walkways, stairs and ramps. It has also been successfully trowel applied to flat roofs for waterproofing. The rubberized formula provides excellent toughness and is fast-drying offering protection from abrasion, corrosion, weather, chemicals and solvents. It has an attractive, textured finish that will not chip, flake or peel, even with impact.

	Application Areas
	· Primed, rusted or new metal whether they be bakkie or trailer load beds, metal roofs or walk ways. 
· Fibre-cement and felt-covered roofs, especially in humid/damp conditions.
· Old weathered torchon bitumen based waterproofing.
· Dynamiq Rubbertex is the ideal coating material for objects where excellent abrasion, water and impact resistance are required.

	Product Features
	· Highly durable, humidity and UV resistant for the harsh Gauteng climate.
· Excellent adhesion to a range of properly prepared substrates.
· Excellent, no mess application properties. Can be applied by spray, brush and trowel to give an attractive textured finish which is abrasion, water, corrosion and impact resistant. 
· Very cost and time effective. 
· Fast drying.

	Product Data
	Resin Base
	Resin bonded rubber crumb

	
	Drying Time
	Touch dry: ± 1 hour

Hard dry: 3-4 hours

	
	Film Thickness
	300-400 microns

	
	Spreading Rate
	1-2 SQM per litre
Although the spreading rate will vary with porosity and type of substrate, for uncoated new surfaces work on 0.5-1 square metres per litre for the first coat and 2-3 square metres per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	
	Surface Appearance
	Texture

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	Trowel, Spray or brush 

	· Thinning
	This product is ready for use un-thinned; thinning will reduce its hiding power. For spray application, thin 20% with QD Thinners. 

	· Cleaning
	· Clean-up application equipment with Xylene or QD Thinners 

	· Application
	· Stir well before use.
· With brush, trowel or spray, apply a generous coat of Dynamiq Rubbertex to the area that needs protecting. Thin for spray 20% with Solumix QD.
· Allow to dry 4-6 hours before recoating.
· Clean up application equipment with Xylene or Solumix QD.
· This product is ready for use un-thinned; thinning will reduce its hiding power.

· Only apply in well ventilated areas and keep away from all ignition sources, flames and sparks.
· Do not eat drink or smoke while applying.
· Do not apply before 09:00 and after 16:00 in the winter.

· Do not apply exterior if it looks like rain will occur with in 4-6 hours of application.


	Surface Preparation
	

	· Rusted Metal
	· Remove any rust, mill scale and greasy substances from metal surface.

· Prime steel with one coat of metal primer.

· Other substrates require no prime coat.

· Apply Dynamiq Rubbertex.

	· New Metal
	· Degrease surfaces with galvanized iron cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water-break free.

· After drying the whole substrate is coated with one coat of  metal primer.
· Apply Dynamiq Rubbertex.

	· Fibre Cement Surfaces and Roofing Felt
	· Remove any flaking, peeling and loose paint from the roof surface.

· Wash off dust and loose particles with a hosepipe and by scrubbing with a hard broom.

· Carry out repairs if required.

· Allow to dry.
· Apply Dynamiq Rubbertex.

	· Primed Metal and Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid. And are not affected by Xylene/Solumix (solvent could soften the previously painted surface). 
· Remove all loose, flaking and bubbling paint.

· Remove all dust, grease, foreign material, fungal and algae growth preferably with a high-pressure cleaner.

· Bare metal areas need to be spot-primed with one coat of metal primer.
· Apply Dynamiq Rubbertex.

	Colour Range and Quantities
	· Black only
· Available in 1 litre, 5 litres and 20 litres.

	Precautions
	· This material is highly flammable and has a flashpoint of 37 degrees Celsius.
· Only apply in well ventilated areas.

· Do not eat drink or smoke while applying.

· Do not coat the inside of containers or water storage tanks with this product.

	Disclaimer
	Dynamiq Intelligent Coatings cannot be held liable if the product fails due to improper surface preparation or application.
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