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	Product Description
	A novel and innovative solvent soluble pure acrylic solution polymer-based interior, exterior satin sheen finish for uncoated slasto, tiles, cement screeds, concrete stone and masonry floor surfaces to protect substrates from rain/sun and medium duty wear and tear.


	Application Areas
	· Low and high-density cement screeds.
· Slasto, stone and uncoated tiles.


	Product Features
	· Impedes fungal growth.
· Excellent adhesion to range of properly prepared slasto, tile and masonry/cement floor substrates.
· Reduces the chance of efflorescence and water absorption.
· Highlights the natural colour of tiles, screeds and slasto.
· Good chemical resistance against a range of domestic/light industrial chemicals.

· Stops staining of the tiles, slasto especially around braai areas.


	Product Data
	Resin Base
	Solvent Soluble Pure Acrylic Polymer

	
	Drying Time
	Touch dry: 1-2 hours
Hard dry: 3-4 hours

	
	Film Thickness
	± 20 microns

	
	Spreading Rate
	Circa 10 SQM per 1 litre per coat
Although the spreading rate will vary with porosity and type of substrate, for uncoated new surfaces work on 8-10 square metres per litre for the first coat and 9-11square metres per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	
	Surface Appearance
	Low Gloss

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	Brush or spray application.

	· Thinning
	This is ready for use un-thinned; thinning with Xylene will reduce its durability.

	· Cleaning
	Application equipment clean-up is with Xylene/Lacquer Thinners.

	· Application
	· With brush, or spray apply a generous coat of Stone Sealer to the area that needs protecting.
· Allow to dry circa 4 hours before recoating.
· Application equipment clean-up is with Xylene/Lacquer.
· Do not apply before 09:00 and after 16:00 in the winter.

	Surface Preparation
	

	· Slasto, Stone and Concrete tiles
· Cement Floors

· Paving
	· Dry (15% moisture Max) uncoated surfaces: Remove all dust, foreign material, Fungal, algae growth- fill and seal all visible cracks with a suitable flexible sealant.
· Apply the first coat thinned 10% with Xylene.
· Allow to dry 4 hours. 
· Apply a second coat.

	Colour Range and Quantities
	· Clear 
· Available in 1 litre, 5 Litres & 20 Litres

	Precautions
	· This product is flammable.

· Use only in well ventilated areas.

· Do not eat, drink or smoke while applying.
· This product continues no toxic substances.

	Disclaimer
	Dynamiq Intelligent Coatings cannot be held liable if the product fails due to improper surface preparation or application.
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