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	Product Description
	· SuperSeal is a low viscosity clear siloxane water repellent that provides hydrophobic properties to alkaline mineral and building substrates. 
· It is based on silane/siloxane and is diluted with organic solvents for better penatration of the substrate.


	Application areas:
	· Plaster-, concrete-, face brick and porous wall and floor tiles.

	Coverage:
	· Four square metres per 1 litre.
· Coverage may vary depending on porosity of the substrate.  
· Best practice is wet on wet application to ensure good penetration  into the substrate.                                                                                                                     

	Directions for use:
	· Ensure the substrate is clean and free from dust and loose particles.
· Ensure that all mold and efflorescence have been removed.
· Shake or stir the product well before use.
· The product requires application by “flooding” the substrate. 
· Apply the product with a hand operated spray bottle.
· Start from the top down on vertical surfaces.
DO NOT APPLY THE PRODUCT WITH A ROLLER OR BRUSH. AVOID ANY FORM OF HIGH SHEAR APPLICATION.
· Apply the first coat. 
· Apply the second coat wet on wet.
· Allow overnight curing before application of any other coating if product is used as a primer.
· After use, seal the container tightly to prevent the remaining product from curing in the container. This is important due to the product reacting with atmospheric moisture.
· After 24 hours curing time you may paint over the product.
DO NOT DILUTE

	Cleaning:
	· It is recommended that Mineral Turpentine be used to clean all spraying application/equipment.
· Run mineral turpentine through your spraying equipment to ensure it reaches and cleans all the internal components.
· Do not attempt to clean spraying equipment with a high
aromatic thinner as this might damage any PVC or plastic parts in the machine.


	Precautions:
	· Before application, be sure to cover windows and other non-absorbent surfaces properly due to the product curing so quick that it will be extremely difficult to remove after a few hours. 
· Wipe off any overspray on window panes immediately using a solvent if necessary.
· Avoid direct contact with eyes.
· Avoid ingesting the product.
· All tile work – wipe access Nano with dry cloth within 10 minutes.
· ALWAYS WEAR A MASK AND GOGGLES WHEN APPLYING THE PRODUCT


	Storage:
	· Store at room temperature in properly sealed containers away from direct sunlight and frost.


	Features and characteristics:
	· Good penetration ability.
· Dries tack free.
· Develops early water repellency.
· This product may be applied to damp surfaces.
· Reacts with atmospheric moisture or pore water in the substrate thereby generating the active ingredient and liberating alcohol.
· Lowers water absorbency in the substrate but still retains a high degree of water vapor permeability.
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