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	Product Description
	A classic alkyd based Universal Undercoat which has been especially formulated to give the best long-term performance for coating on a wide range of prepared household surfaces such as doors, window frames, down pipes etc. 

	Application Areas
	· Hardboard and fibre cement boards.
· Primed metal and wooden substrates.
· As a transition coat when overcoating an enamel surface with a water-based paint.
· As a wood primer for raw wood.



	Product Features
	· A high-hiding power, low gloss finish for Interior and Exterior use 
· Excellent adhesion.
· Excellent, no mess application properties.
· Can be cleaned with normal house hold-cleaners on a regular basis.

	Product Data
	Resin Base
	Synthetic Alkyd resin

	
	Drying Time
	Touch dry: 2-4 hours
Hard dry: 16-18hours

	
	Film Thickness
	± 30 microns

	
	Spreading Rate
	 8-10 SQM per 1 litre
Although the spreading rate will vary with porosity and type of substrate, for uncoated new surfaces work on 7-9 square metres per litre for the first coat and 9-11 square metres per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	
	Surface Appearance
	Low Gloss

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	· Brush, roller or spray application.

	· Thinning
	This is ready for use un-thinned; thinning with Turpentine will reduce its hiding power.

	· Cleaning
	Application equipment clean-up with Turpentine (White spirits)

	· Application
	· With brush, roller or spray, apply a generous coat of Dynamiq Universal Undercoat to the area that needs protecting.
· Allow to dry overnight before recoating.
· Do not apply before 09:00 and after 16:00 in the winter.

	Surface Preparation
	

	· Rusted Metal
	· Remove any rust and mill scale from steel surface.

· Affected areas need to be cleaned back to bright metal 

· Apply one coat of solvent-based metal red oxide primer, leave to dry overnight then apply a coat of Dynamiq Universal Undercoat. Allow to dry overnight.
· Apply two coats of enamel or water-based Acrylic.

	· New Metal
	· Degrease surfaces with an industrial degreaser to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free.

· After drying apply one coat of solvent-based red oxide primer, leave to dry overnight. Apply a coat of Dynamiq Universal Undercoat and allow to dry overnight.
· Apply two coats of enamel or water-based Acrylic 


	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid.

· Remove all loose, flaking and bubbling paint.

· Remove all dust, grease, foreign material, fungal and algae growth.

· If powdery or friable, seal with Dynamiq Bonding Liquid.
· Prime with alkali resistant primer.

· Apply a coat of Dynamiq Universal Undercoat. 
· Apply two coats of enamel or water-based acrylic.

	· Wood and Wood Fibre Boards
	· Sand surface until smooth.

· Apply one coat of Dynamiq Universal Undercoat.
· Apply two coats of enamel or water-based acrylic.

	Colour Range and Quantities
	· White
· Available in 1 litre, 5 litres and 20 litres.

	Precautions
	· This product is flammable.

· Use only in well ventilated areas.

· Do not eat, drink or smoke while applying.
· This product continues no toxic substances.

	Disclaimer
	Dynamiq Intelligent Coatings cannot be held liable if the product fails due to improper surface preparation or application.
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