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	Product Description
	A traditional alkyd-based corrosion resistant and rust-retarding primer which has been especially formulated to give good long-term performance when used as part of system. For use on mild steel and weathered galvanised iron. 

	Application Areas
	· Mild steel and weathered galvanized iron 

	Product Features
	· Excellent corrosion protection and rust resistance.
· Excellent adhesion.
· Excellent recoatablity with decorative under coats and top coats.
· Excellent no mess application properties.

	Product Data
	Resin Base
	Synthetic Alkyd resin

	
	Drying Time
	Touch dry: 2-3 hours
Hard dry: 16 hours

	
	Film Thickness
	± 30 microns per coat 2 coats required 

	
	Spreading Rate
	 6-8 SQM per 1 litre
Although the spreading rate will vary with type of substrate

	
	Surface Appearance
	Matt 

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	Brush (Mostly), or spray application.

	· Thinning
	This is ready for use un-thinned; thinning with Mineral Turpentine (White Spirits) will reduce its hiding power.

	· Cleaning
	Application equipment clean-up is with Mineral Turpentine

	· Application
	· With brush or spray, apply a generous coat of Dynamiq Zinc Phosphate Primer to the area that needs protecting.
· Allow to dry at least 8 Hours before top-coating. Allow longer drying time in cold winter months.
· Application equipment clean-up is with Mineral Turpentine.
· Do not apply before 09:00 and after 16:00 in the winter.

	Surface Preparation
	

	· Rusted/New Metal
	· Remove any rust and mill scale from steel surface.

· Affected areas need to be cleaned back to bright metal. 

· Apply one coat of Dynamiq Zinc Phosphate Primer and leave to dry over night  before over-coating with a suitable undercoat or top coat.

	Colour Range and Quantities
	· Available in olive green only  
· Available in 1, 5 and 20 litres 

	Precautions
	· This product is flammable.

· Use only in well ventilated areas.

· Do not eat, drink or smoke while applying.

	Disclaimer
	Dynamiq Intelligent Coatings cannot be held liable if the product fails due to improper surface preparation or application.
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